***Technical Data Sheet***

|  |  |  |  |
| --- | --- | --- | --- |
| No | CHARACTERISTIC | Accepted Limit | METHOD |
| 1 | Appearance  | Yellowish Brown |  |
| 2 | Oil content % | 20 - 30 | ASTM D-721 |
| 3 | Kinematic Viscosity @100 ͦ C | 5 - 7 | ASTM D-445 |
| 4 | Drop Melting Point | 45 - 55 | ASTM D-127 |
| 5 | Congealing point  | 40 - 50 | ASTM D-938 |

*Residue Wax (Foots Oil)*